Tiekėjų klausimas:
Re 2 Layers Rip Stop Fabric 


1. Abrasion  (≥ 200 000)   is too high.   Change the abrasion resistance back to the same as it was  for previous 
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	Abrasion 12 kPa 
	≥ 100 000 



2. [bookmark: _Hlk207608538]Tensile strength. Normally WARP direction is higher; should it be  ≥ 750  / ≥ 500    
Instead of   ≥ 500/   ≥ 750  

3. TEAR Strength .  This indicator should be sufficient for fabric of this weigh
	TEAR Strengh, N 
warp 
Weft 
	≥ 40 
≥ 40 





Atsakymas:


1.,3. Universalios striukės audinio paviršinis tankis yra mažesnis, todėl ir atsparumas dilimui ir plyšimui gali būti mažesnis.

2.  Didžiosios jėgos rodiklius pakoreguosime sekančiai: Metmenų kryptimi ≥750; ataudų ≥ 500
