Appendix 1 to Annex 2 to the Purchase Conditions (In case of differences in interpretation the Lithuanian text shall prevail)

TECHNICAL SPECIFICATIONS FOR THE PROPOSED BALLISTIC PROTECTIVE SUNGLASSES

(applicable to Part 1)

By submitting a tender for a purchase, the supplier certifies that, the object to be purchased will meet the following requirements:

| Technical specification item | Required technical characteristics of the goods | Possible value | Specific values for the product indicators offered by the supplier* | Supporting documents. |
| --- | --- | --- | --- | --- |
| I. | GENERAL PROVISIONS |  |  |  |  |
| 2. | The glasses are designed to provide eye protection for soldiers on combat missions | Yes or no |  | - |
| 4. | The glasses shall be manufactured to comply with the ballistic protection and optical class standard MIL-PRF-32432A or equivalent for Class 1 protective glasses. | Class 1 (spectacles) |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 5. | The term of the product quality guarantee shall be not less than 12 (twelve) months under conditions of active operation starting from the date of issue of the goods from the Buyer’s warehouse, 24 (twenty-four) months starting from the date of the signing of the documents of acceptance of the goods into warehouse. | Specify the exact duration of the guarantee |  | - |
| II. | TECHNICAL REQUIREMENTS |  |  |  |  |
| 6. | Glasses must provide good visibility and the lenses must be made of a highly transparent, durable, shatterproof material (polycarbonate or equivalent in terms of functionality). | Specify |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 7. | The glasses must be compatible with Advanced Combat Helmet (ACH), Modular Integrated Communications Helmet (MICH), Future Assault Shell Technology (FAST) ballistic helmets used in the Lithuanian Armed Forces. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 8. | The frame of the glasses shall be resistant to harsh and extreme environmental conditions and shall be made of black or yellowish-brown (colour to be agreed at the time of the working sample), durable, flexible thermoplastic polyurethane (TPU) or equivalent material. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 9. | No additional tools or equipment shall be required for the replacement or removal of spectacle components such as lenses, nose piece, as specified in MIL-PRF-32432A Standard clause 3.6.4 or equivalent. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 10. | The colour transmittance of glasses shall comply with the limits specified in accordance with clause 3.8.5.4 of standard MIL-PRF-32432A or equivalent. | Specify x; y =? |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.9.4) provide a reference to the document, page, clause |
| 11. | The lenses of glasses shall not be colour-fused as specified in clause 3.8.5.8 of standard MIL-PRF-32432A or equivalent. | Yes or no |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.9.8) provide a reference to the document, page, clause |
| 12. | Glasses shall not break or otherwise change shape when subjected to the temperatures specified in clause 3.9.5.1 of standard MIL-PRF-32432A or equivalent. | 72 h (-60F°; 160 F°) |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 13. | Glasses shall not break or otherwise change shape when exposed to sunlight as specified in clause 3.9.5.2 of standard MIL-PRF-32432A or equivalent. | 200 h |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 14. | Glasses shall not break or otherwise change shape when exposed to moisture as specified in clause 3.9.5.3 of standard MIL-PRF-32432A or equivalent. | 240 h |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 15. | Glasses shall not break or otherwise change shape, although they do not have adequate support points as specified in clause 3.9.5.4 of standard MIL-PRF-32432A or equivalent. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 16. | Glasses shall be flame retardant at a rate higher than 76 mm per minute and shall meet the ignition/flame retardancy requirements of ANSI Z87.1 2015 or equivalent standards as defined in clause 3.14.1 of standard MIL-PRF-32432A, or equivalent standard. | ≤76 mm/min |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.18) provide a reference to the document, page, clause |
| 17. | Textile products supplied with protective glasses shall be resistant to mould for at least 6 months of active use or 60 months of storage and shall comply with clause 3.8.2 of standard MIL-PRF-32432A or equivalent. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 18. | Glasses shall provide eye protection against ballistic fragments, splinters, detonation of explosive charges, mechanical eye damage, dust, wind, liquids, in all components of glasses, as specified in clause 3.8.4 of MIL-PRF-32432A, or equivalent standard. | Yes or no |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.8.4) provide a reference to the document, page, clause |
| 19. | Glasses shall provide good visibility in all climatic conditions and the lenses shall be coated with a rust-resistant coating in accordance with the requirements of clause 3.8.5.11 of MIL-PRF-32432A, or equivalent standards. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 20. | The protective glasses system shall have an elastic adjustable glasses fitting/locking strap for effective and comfortable use by the soldier. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 21. | Glasses shall intercept not less than 99,9 % of harmful ultraviolet (UV-A, UV-B) rays in accordance with the requirements of clause 3.8.5.9 of MIL-PRF-32432A, or equivalent standard. | ≥ 99.9% |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.9.9) provide a reference to the document, page, clause |
| 22. | Glasses shall be resistant to acids and alkalis and shall comply with clause 3.8.3 of MIL-PRF-32432A or equivalent standard. | Yes or no |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.7.3) provide a reference to the document, page, clause |
| 23. | Glasses shall have maximum scratch resistance in accordance with clause 3.8.5.10 of standard MIL-PRF-32432A or equivalent. | Specify % |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.10) provide a reference to the document, page, clause |
| 24. | Soldiers with visual impairments shall be able to insert a (Rx) optical corrective lens holder into their glasses that is compatible with the glasses and shall have all necessary adaptors. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 25. | Glasses shall ensure a wide field of vision in all directions when lying down and standing, in accordance with the requirements of clause 3.8.5.7 of MIL-PRF-32432A, or equivalent standard. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 26. | The glasses shall be comfortable to wear without discomfort in accordance with clause 4.15.4 of MIL-PRF-32432A or equivalent standard. | Yes or no |  | - |
| 27. | The glasses must be new and without any defects. | Yes or no |  | - |
| 28. | The methods for verifying the requirements are defined in Table VI of standard MIL-PRF-32432A, in accordance with clause 4.2, or its equivalent. | Yes or no |  | - |
| 29. | The user guide for the glasses must be available in Lithuanian or English. | Specify |  | - |
| 30. | Protective sunglasses set: - glasses frame; - elastic, adjustable glasses strap; - protective clear lens; - protective dark lens; - adjustable nose support; - zipped storage and transport case for glasses; - cleaning product (wipe) for protective lenses; - user manual for the protective goggles (in Lithuanian or English). | Specify |  | - |
| 31. | The ballistics of the lenses shall be such that they pass the test of a vertical impact of 0,15 calibre (0,0381 mm) in diameter once on the right and once on the left side of the base of the spectacle lenses, 5,85 (± 0,15) grains (0,38 grams), T37 shaped fragment, at a velocity of 700 to 725 feet per second (213,36 to 220,98 m/s) in accordance with clause 4.8.4 of MIL-PRF-32432A or equivalent standard. | Specify |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.8.4) provide a reference to the document, page, clause |
| 32. | Protective glasses shall have an elastic head strap with a length adjuster to ensure a comfortable fit on the head and, in the event of impact, jumping or other sudden action, a secure hold and to protect the eyes from imminent danger. An adjustable strap to hold the glasses in place shall be provided in accordance with clause 3.5.1.1 of MIL-PRF-32432A or an equivalent standard. | Yes or no |  | - |
| 33. | The glasses shall have a soft (possibly replaceable) nose rest that adapts well to the profile of the soldier's nose. When wearing the glasses, the temples of the glasses shall not press and dig into the soldier's head, but shall also securely hold the glasses in place without the support strap during walking and running. The nose support shall be easily adjustable for proper and comfortable wearing of in accordance with clause 3.10.3 of MIL-PRF-32432A or equivalent standard. | Yes or no |  | - |
| 34. | Protective glasses for transport, wear and protection against dust and dirt shall be supplied with a case made of strong fabric, with a zip fastening and with at least two compartments for storing the protective lenses. At least two straps on the back of the case for attachment to the belt and equipment. The attached case shall hold securely during active movement. | Yes or no |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 35. | The glasses shall be supplied with a clear lens in accordance with clause 3.8.5.1 of MIL-PRF-32432A or equivalent. A photopic transmission of light of not less than 89 per cent. | ≥89% |  | provide a test report from a laboratory accredited according to international standards (tests according to MIL-PRF-32432A 4.9.1/4.9.2) provide a reference to the document, page, clause |
| III. | OPTICAL CORRECTION LENS HOLDER |  |  |  |
| 36. | The holder must be sturdy and the frame durable | Yes or no |  | - |
| 37. | The field of vision of the holder shall be wide. The colour of the frame of the holder shall not be distracting or distort the view. | Yes or no |  | - |
| 38. | Must be suitable for lenses of at least ± 6 dioptres made of polycarbonate or other resistant material. | Specify |  | provide a product description and/or the manufacturer's technical documentation and/or a declaration/confirmation from the manufacturer of the glasses provide a reference to the document, page, clause |
| 39. | The holder must be suitable for sunglasses and be fixed. | Yes or no |  | - |
| 40. | The corrective lenses must be safely and securely pressed into place. | Yes or no |  | - |
| IV. | ACCEPTANCE AND LABELLING |  |  |  |
| 41. | Instructions for use and care must be included in Lithuanian or English in each package supplied. | Specify |  | - |
| 42. | Each product is labelled where indicated: the manufacturer’s name or trademark; for imported goods, the country of origin of the goods, if this is not the same as the country in which the manufacturer is registered; the product name, article or model; protective glasses components such as the frame and lenses are marked with markings that meet the required standards; date of manufacture; the labelling particulars shall be of sufficient size to permit easy reading and understanding of the information provided. | Yes or no |  | - |
| 43. | Safety glasses sets are packed in cardboard boxes. The packaging shall comply with the minimum environmental criteria set out in Annex 2, Chapter II 'Packaging' of Annex 2 to the 'Description of the Procedure for the Application of Environmental Criteria in Green Procurement' approved by Order No D1-508 of the Minister of the Environment of the Republic of Lithuania on 28 June 2011. | Yes or no |  | - |
| 44. | Packages shall be labelled with the following particulars: manufacturer’s name, address (for goods made in Lithuania); for imported goods, the country of origin of the goods, if this is not the same as the country in which the manufacturer is registered; the importer’s name or trade mark and address for imported goods; product name, article or model; batch and consignment indexes; size, colour (if more than one colour is supplied); quantity; date of manufacture; contract No. and date; NSN code issued by the Lithuanian Armed Forces or the manufacturer's existing NSN code if the products have one. | Yes or no |  | - |
| 45. | Products shall be accepted on the basis of an agreed and approved working sample. Two protective glasses shall be submitted for approval of the working samples, together with documentation (descriptions and test reports of the materials used by the manufacturer, test reports from certified laboratories). | Yes or no |  | - |

*The supplier must indicate the specific values of the technical characteristics to which the goods offered conform and which are indicated in the laboratory test reports or other copies of documents submitted with the tender.

_________________________